## Slide 1: Mayday! Mayday!: Investigating the Performance of Radio Cables in High Temperature Environments
Shelley Jin
Advisor: Michelle Donnelly
Engineering Laboratory, Fire Research Division, Fire Fighting Technology Group

## Slide 2: Introduction
Technology constantly advancing
Greater use of electronic devices
  PASS
  SCBA
  Thermal Imaging
  Radios

## Slide 3: Existing Standards
Current official standards on radio performance:
  NFPA1221 8.3.5.4: “Mobile radios and associated equipment shall be manufactured for the environment in which they are to be used”
  NFPA1221 8.3.6.2: “Portable radios shall be manufactured for the environment in which they are to be used and shall be of a size and construction to allow their operation with one hand

## Slide 4
What is “environment”?

## Slide 5: Current Situation
NFPA1802 radio code in development
  Research directly contributing
Test current equipment
  Examine performance
  Recommend requirements/testing methods

## Slide 6: Project Scope
Looking specifically at radio cables
  Protected radios resilient
  Cable = weakest link?

## Slide 7: Thermal classes
Thermal Class | Max Time (min) | Max Temp (oC/oF) | Max Flux (kW/m2)
I | 25 | 100/212 | 1
II | 15 | 160/320 | 2
III | 5 | 260/500 | 10
IV | <1 | >260/500 | >10

## Slide 8: Flow Loop
Testing Chamber
Heater
Blower
Loading Platform
8’2” or ~2.5m tall

## Slide 9: Chamber Instrumentation
Heat Flux Gauge
Bi-directional Velocity Probe
Thermocouple Tree
Radio Signal
Transmitter

## Slide 10: Previous Tech Tests

## Slide 11: Cables Tested
Tested three cable types: B, D, X
  D & X: same year & manufacturer
    D: standard temperatures
    X: extreme temperatures
  B: different manufacturer
  Expected Performance: X>D>B

## Slide 12: Cable Testing Setup
*
*
*
2 TC at each *
One touching, one in air

## Slide 13: Results
Type |  | Class II | Class III
B | 1 | Passed | Failed 88 sec in
 | 2 | Passed | Failed 128 sec in
 | 3 | N/A | Failed 175 sec in
D | 1 | N/A | Failed 168 sec in
 | 2 | Passed | Failed 165-180 sec in
X | 1 | N/A | Passed
 | 2 | Passed | Passed
Note: performed a baseline Class I Test for B1

## Slide 14: Cable Comparisons
Cable B
Cable D
Cable X

## Slide 15: Close Up of Damage
Cable B
Cable D

## Slide 16: Testing Chamber—Heat Flux
Relative Standard Deviation for tests ~3%

## Slide 17: Cable Temperatures

## Slide 18: Regular Radio Behavior
On
Off

## Slide 19: Abnormal Radio Signal
Control
Cable B2

## Slide 20: Conclusions
Mixed performance with current equipment
Meeting extreme temperature performance feasible
Recommend NFPA1802 Committee to include Thermal Class III testing
Flow loop produces repeatable test environment

## Slide 21: Future Plans
Test different soak conditions
Examine speaker microphone
Introduce moisture—observe humidity